## Slide 1
Test of mirror painting & clear fiber
Chendi Shen
2017.04.13

## Slide 2
Gain of the SiPM (SPE)
104.1pvs=1PE
Preamplifier
50Ω for oscilloscope

## Slide 3
1. Test of mirror painting
Laser source
SiPM+ Preamplifier
WLSF
Waveform sampling oscilloscope
Get the data of Npe
Aluminum
or
Nothing
or
Silver shine
Test in the dark box
Light spot
Fibers were fixed on the light spot
trigger
For laser source:
420 nm
1 MHz
For SiPM:
Gain :
104.1pWb=1 pe
Voltage=25.0 V
For the fibers:
50 cm
Have been polished
Filter sheet
laser intensity monitoring
spectroscope

## Slide 4
WLSF（Y11）+ Al
Npe=

## Slide 5
WLSF（Y11）（after polishing to remove Al）
Npe=

## Slide 6
WLSF（Y11）+ silver shine 415001
Npe=

## Slide 7
Compared results
 | Y11
No mirror painting | 85.6
Al | 97.4 (+13.8%)
Silver shine 415001 | 110.7 (+29.3%)
(Al —— light leakage)
So it is not the real proformance of this method. It should be better than 13.8%.

## Slide 8
2. Test of clear fiber
Laser source
SiPM+ Preamplifier
clear fiber
Waveform sampling oscilloscope
Get the data of Npe
Light spot
trigger
For laser source:
420 nm
1 MHz
For SiPM:
Gain :
143.6pWb=1 pe
Voltage=25.0 V
For the fibers:
1m, 2m, 3m, 4m, 5m, 7m and 9m
Have been polished
Filter sheet
laser intensity monitoring
spectroscope

## Slide 9
2.1 measure the light loss due to bending
Bending tool
1m of clear fiber

## Slide 10
No bending=
=

## Slide 11
φ=
=

## Slide 12
=
=

## Slide 13
=
Chart: Npe with different bending
| no bending | 20 | 11 | 8 | 6 | 4 | 2.7
系列 1 | 119.3 | 116.4 | 115.9 | 116.8 | 119 | 114.3 | 113
The effect of bending on the clear fiber can be ignored

## Slide 14
2.1 measure the light loss due to length
End of the fiber

## Slide 15
=
Background (9m)

## Slide 16
=
Background (7m)

## Slide 17
=
Background (5m)

## Slide 18
=
Background (4m)
As the signal is too large, so when the length is less than 4m, we removed the preamplifier.
That means 1.041pVs=1PE

## Slide 19
=
Background (3m)

## Slide 20
=
Background (2m)

## Slide 21
=
Background (1m)

## Slide 22
Two kinds of exponential fitting with different function