EC and SPD Updates
The SoLID EC Working Group
SoLID Collaboration Meeting
October 13-14, 2017

---
Outline
Prototype shashlyk module overview, problem with PMT gain.
Cosmic test preliminary results on LASPD timing resolution
Progress on reproducing the Ecal simulation, mostly on pre-lead thickness (Ye/Syracuse); Note: from March and June meetings: Birk’s effect and photoelectron statistics (March meeting) have to wait.
Brief progress on LASPD segmentation simulation
Not much progress to report this time on testing clear fiber attenuation (Chendi/THU) and fiber reflective coating ongoing (Chendi/THU + Cunfeng+Ang/SDU)
Preparation for CD0, CD1?

---
Shashlyk prototype and light yield overview
Proto-type	scintillator	lead	reflective layer	WLS fiber	WLS fiber end	module side	cosmic vertical test Npe	cosmic horizontal test Npe	PMT gain method
SDU1	Kedi original	US	printer paper	BCF91A	none	Tyvek→ TiO2	224→ 254	48 → N/A**	SPE/SDU
SDU2	Kedi new	Chn	printer paper	BCF91A	Chn silver-plating	Tyvek→ TiO2*	427 → 383*	83 → N/A**	SPE/SDU
SDU3	Kedi new	US	printer paper	Y11	Chn silver-plating	TiO2+glue (1/1)	491	107	SPE/SDU
THU1	Kedi original	Chn	mirror mylar (reflective)	Y11	Italian silver shine	TiO2 (Kedi)	430-470	96	not measured
THU2	Kedi new	Chn	powder paint (喷塑） (diffusive)	BCF91A	Italian silver shine	Tyvek wrapping (now)	748	90-103	SK/SP (Beijing Hamamatsu)
* TiO2 side-paint was not as good as SDU1 ** could not finish before shipping to JLab
       Yields 500/200 layers for MIP → 1666 p.e./GeV electron, factor 2-3 lower than LHCb or ALICE → 833 p.e./GeV if using clear fibers → 3.5% in δE/E due to photoelectron statistics
SDU is planning to construct SDU4.

---
PMT Gain Puzzles
PMT gain method:
1) SPE/SDU: SPE determined at high HV, then increase LED light so signal is high enough to see at low HV, then measure signal vs. HV and use signal to calculate gain for all HV values – should be the most reliable (SDU PMT also have manufacturer’s SK/SP data but not sure what base was used).
2) THU SK/SP: measured at Beijing Hamamatsu with the SK/SP ratio, base changed but was told base is “identical to” the one used for testing at THU.
3) THU took their PMT to Beijing IHEP and measured the SPE at high HV (with the same base), then calculate gain at low HV – found gain to be 2/3 of the SK/SP method. This means the vertical yield for SDU2 is ~1000 instead of 750 – factor two difference between SDU and THU for similar material construction
Ongoing effort:
1) SDU will take their PMT to Beijing IHEP for comparison of the two SPE facilities;
2) THU will take their PMT to SDU for comparison of the two SPE facilities;
3) Both need to do a thorough uncertainty analysis;
4) Would be good to see both SPE and main peak (horizontal test) but both SDU and THU do not have the proper PMT. Can we do so by adding a filter?

---
JLab Test Lab Cosmic Runs (Ye Tian/SDU + Jixie/UVa)
LASPD time resolution test
PMT labeling:
t0
t3
t1
LASPD
t4
t2
t5
Wide side
Narrow side
SPD about 55 cm long

---
June meeting
No correction from GEM hit position yet. Trigger bars are 5cm wide
Readout from only the wide side:
Readout from only the narrow side:
198ps
184ps

---
Now, with GEM x-binning and correction

---
Now, with GEM x-binning and correction

---
JLab Test Lab Cosmic Runs (Ye Tian/SDU + Jixie/UVa)
The timing resolution (t0+t3+t2+t5)/4-t4 was measured to be 184ps (see previous two slides) when reading out from the wide side with the event hitting the left-most side (similar to the SoLID condition). We take out the resolution of the trigger bars (82ps for each of the t0,t3,t2 and t5), the resolution for t4 is 170ps. Eventually this dominates the TOF for the LA particles (since the other timing for the coincidence is from MRPC which has a 60-80ps resolution depending on the rate, and is still been improved on) – note: SIDIS requires 150ps.
More timing analysis is still going on. It was found cutting on y position may improve timing.
Also need to determine/check THU1 light yield for the horizontal position, with SDU’s PMT (for which gain was determined with the SDU/SPE method), or with UVa’s XP2262 PMT (used for preshower test at UVa and had SPE and the 90 p.e. peaks on the same spectrum.)
Will be good to measure LASPD’s light yield, but this also need to know the PMT gain and thus the SDU PMT.

---
ECal Simulation
Last meeting (June), found huge effect of prelead thickness on energy resolution. What’s the effect on PID?

---
FAEC 2Xo prelead
LAEC 2Xo prelead

---
Now doing trigger simulation with backgrounds.
Also doing PVDIS PID simulation.
still need to add Birk effect, Nphe statistics, etc. Will Birk effect improve pion PID?

---
LASPD Simulation (Sanghwa’s work)

---
Looks like x60 azimuthal segmentation is no longer good enough. We need 90 or 120 segmentations. – challenges: higher cost; smaller side for readout (lower light yield?); very tight room if doubling need of light guides and FMPMTs.
The other solution is to have two LASPDs: a thin one with WLS fiber embedding (similar to FASPD) for photon rejection; and a thick one with 60 segmentation for timing (this can even be made thicker to improve timing).
Note from the meeting: we were told Sanghwa’s simulation is probably more reliable than Zhihong’s because the newer GEMC is more complete (than Zhihong’s).

---
Preparation for CD0 and CD1
Continue shashlyk prototyping (SDU, THU), figure out the gain puzzle. If 1000 → Okay. If 500 → not okay and we need to figure out how to reach the light yield of LHCb.
Continue cosmic test and analysis – finalize LASPD timing data; determine light yield of LASPD; determine relative yield of THU1 module;
Continue LASPD simulation, if confirming more segmentation is needed, need to test new prototype and/or more simulation for a second LASPD.
Continue clear fiber test – previously only THU, but SDU will also start.
Continue simulation on triggering, then proceed to other aspects (Birk effect, photon statistics, photon collection, etc.).
Need to fully understand shashlyk data from Hall A test, then plan for a full-cluster beam test (Fermilab or Beijing).
Support design from ANL has been suspended for a while due to budget issues.
(From March meeting: LHCb will dismount their preshower in 2019, (in Dec 2016) asked us if we are interested.)

---
ECal + SPD cost estimate (June 2017)
Item	2014	2017
Shashlyk	$2,997,657 (1800 modules Russian IHEP)	China using 0.1454USD/Y: / $3,460,567 (1800 modules); / $3,630,323 (5% extra) / +US $40k lead (material only)
Preshower	$280,800 (1800 modules Russian IHEP)
SPD (Eljen)	FA: $54,900; / LA: $34,680	FA: $58,620 / LA: $37,440
HV/CAEN	$1,026,624	$365,015 (newer, lower cost modules)
PMT/Hamamatsu	$885,600 (5% spare incl., MAPMT overestimated); FMPMT not quoted; plus MAPMT base/preamp	$797,510 (5% spare included), plus 128 units of MAPMT base/preamp at $200 each(?) → $825k?
Fiber (Saint Gobain)	$700k (~$1/m, 200kmWLS, 520km clear)	$996.5k ($1.8/m WLS 192km, $1.25m clear 520km)
Fiber (Kuraray)	$64k ($2/m 23.5km clear, $3.2/m 6800m WLS)	$82,281 ($4.67/m WLS 6.8km; $2.15/m clear 23.5km)
Fiber connectors	$365k	$420k (incl. 5% spare)
Total	$6,411k	$6,455k

---
Ecal Simulation (Ye Tian/Syracuse)
support structure
Ye is using the following function to fit simulation:
{ %delta E }over{ E }={ p_0 }over{ sqrt{E} } oplus p_1 oplus { p_2 }over{ E }